IEC Standard Caledonian Offshore & Marine Cables

MariTox Marine Flame Retardant Power & Control Cables

www.caledonian-cables.co.uk

MTX400 0.6/1 kV HEPR Insulated, LSOH (SHF1) Sheathed, Screened Flame Retardant Power & Control Cables (Multicore)

Application

These cables are used for fixed installations on ships and offshore units in all locations and on open deck. The good screening qualities of the copper braid also reduce radio interference and electrical influences to electronics installations. These cables are flame retardant, low smoke & halogen free.

Standards

	DIN 89160/98

	IEC 60092-353

	IEC 60332-1

	IEC 60332-3-22

	IEC 60754-1/2

	IEC 61034

Stranded Copper Conductor HEPR Insulation Lapping/Extruded Filler Copper Wire Braid Screen LSOH (SHF1) Sheath

Construction

- Conductors: Class 2 stranded copper conductor.

- Insulation: HEPR.

- Inner Covering: Lapping or extruded filler.

- Overall Screen: Copper wire braid.

- Outer Sheath: LSOH (SHF1).

Core Identification

Two cores: Black, Blue.

Three cores: Black, Blue, Brown.

Four cores: Black, Blue, Brown, Black.

Five cores: Black, Blue, Brown, Black, Black.

Multi cores: All cores natural coloured, printed with numbers, starting in center with number 1. Cables with 3 cores and more also with green/yellow core (has to be stated in order).

www.addison-cables.com

ADDISON	27

IEC Standard Caledonian Offshore & Marine Cables

MariTox Marine Flame Retardant Power & Control Cables

www.caledonian-cables.co.uk

Mechanical and Thermal Properties

Bending Radius for Fixed Installations: 6×OD Temperature Range: -20℃ ~ +75℃

Dimensions and Weight

| Part No. | Construction No. of cores×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MTX400-1G7MZ1-R-2C1.5 | 2×1.5 | 0.7 | 1.2 | 11.3 | 180 |
| MTX400-1G7MZ1-R-2C2.5 | 2×2.5 | 0.7 | 1.2 | 12.3 | 220 |
| MTX400-1G7MZ1-R-2C4 | 2×4 | 0.7 | 1.3 | 13.3 | 280 |
| MTX400-1G7MZ1-R-2C6 | 2×6 | 0.7 | 1.3 | 15.3 | 380 |
| MTX400-1G7MZ1-R-2C10 | 2×10 | 0.7 | 1.4 | 17.0 | 500 |
| MTX400-1G7MZ1-R-2C16 | 2×16 | 0.7 | 1.5 | 19.5 | 710 |
| MTX400-1G7MZ1-R-2C25 | 2×25 | 0.9 | 1.6 | 22.0 | 1020 |
| MTX400-1G7MZ1-R-3C1.5 | 3×1.5 | 0.7 | 1.2 | 11.8 | 210 |
| MTX400-1G7MZ1-R-3C2.5 | 3×2.5 | 0.7 | 1.2 | 12.8 | 260 |
| MTX400-1G7MZ1-R-3C4 | 3×4 | 0.7 | 1.3 | 13.8 | 330 |
| MTX400-1G7MZ1-R-3C6 | 3×6 | 0.7 | 1.3 | 15.8 | 450 |
| MTX400-1G7MZ1-R-3C10 | 3×10 | 0.7 | 1.4 | 18.0 | 620 |
| MTX400-1G7MZ1-R-3C16 | 3×16 | 0.7 | 1.5 | 20.5 | 870 |
| MTX400-1G7MZ1-R-3C25 | 3×25 | 0.9 | 1.7 | 23.8 | 1280 |
| MTX400-1G7MZ1-R-3C35 | 3×35 | 0.9 | 1.8 | 26.5 | 1680 |
| MTX400-1G7MZ1-R-3C50 | 3×50 | 1.0 | 2.1 | 29.8 | 2180 |
| MTX400-1G7MZ1-R-3C70 | 3×70 | 1.1 | 2.0 | 34.8 | 3020 |
| MTX400-1G7MZ1-R-3C95 | 3×95 | 1.1 | 2.3 | 39.3 | 4050 |
| MTX400-1G7MZ1-R-3C120 | 3×120 | 1.2 | 2.5 | 43.3 | 5000 |
| MTX400-1G7MZ1-R-4C1.5 | 4×1.5 | 0.7 | 1.2 | 12.3 | 240 |
| MTX400-1G7MZ1-R-4C2.5 | 4×2.5 | 0.7 | 1.3 | 14.3 | 300 |
| MTX400-1G7MZ1-R-4C4 | 4×4 | 0.7 | 1.3 | 15.3 | 430 |
| MTX400-1G7MZ1-R-4C6 | 4×6 | 0.7 | 1.4 | 17.0 | 540 |
| MTX400-1G7MZ1-R-4C10 | 4×10 | 0.7 | 1.5 | 19.5 | 780 |
| MTX400-1G7MZ1-R-4C16 | 4×16 | 0.7 | 1.6 | 22.3 | 1090 |
| MTX400-1G7MZ1-R-4C25 | 4×25 | 0.9 | 1.8 | 26.3 | 1630 |
| MTX400-1G7MZ1-R-4C35 | 4×35 | 0.9 | 1.9 | 29.0 | 2120 |
| MTX400-1G7MZ1-R-4C50 | 4×50 | 1.0 | 2.0 | 33.0 | 2750 |
| MTX400-1G7MZ1-R-4C70 | 4×70 | 1.1 | 2.3 | 38.8 | 3900 |
| MTX400-1G7MZ1-R-4C95 | 4×95 | 1.1 | 2.5 | 43.8 | 5160 |

28	ADDISON	www.addison-cables.com

IEC Standard Caledonian Offshore & Marine Cables

MariTox Marine Flame Retardant Power & Control Cables

www.caledonian-cables.co.uk

| Part No. | Construction No. of cores×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MTX400-1G7MZ1-R-5C1.5 | 5×1.5 | 0.7 | 1.3 | 13.3 | 290 |
| MTX400-1G7MZ1-R-5C2.5 | 5×2.5 | 0.7 | 1.3 | 15.3 | 400 |
| MTX400-1G7MZ1-R-7C1.5 | 7×1.5 | 0.7 | 1.3 | 14.3 | 380 |
| MTX400-1G7MZ1-R-10C1.5 | 10×1.5 | 0.7 | 1.3 | 17.0 | 450 |
| MTX400-1G7MZ1-R-12C1.5 | 12×1.5 | 0.7 | 1.4 | 18.0 | 500 |
| MTX400-1G7MZ1-R-14C1.5 | 14×1.5 | 0.7 | 1.4 | 18.5 | 560 |
| MTX400-1G7MZ1-R-16C1.5 | 16×1.5 | 0.7 | 1.4 | 19.8 | 630 |
| MTX400-1G7MZ1-R-19C1.5 | 19×1.5 | 0.7 | 1.5 | 20.5 | 710 |
| MTX400-1G7MZ1-R-24C1.5 | 24×1.5 | 0.7 | 1.6 | 24.0 | 880 |

www.addison-cables.com

ADDISON	29