IEC Standard Caledonian Offshore & Marine Cables

MariTox Marine Flame Retardant Power & Control Cables

www.caledonian-cables.co.uk

MTX400 0.6/1 kV XLPE Insulated, LSOH (SHF1) Sheathed Flame Retardant Power & Control Cables (Multicore)

Application

These unarmoured power & control cables are used on board of ships in all locations for fixed installations not subject to mechanical risk complying with IEC standards 60092-352. These cables are flame retardant, low smoke & halogen free.

Standards

	IEC 60092-350/351/353/359

	IEC 60332-1

	IEC 60332-3-22

	IEC 60754-1/2

	IEC 61034

Stranded Copper Conductor XLPE Insulation

LSOH (SHF1) Sheath

Construction

- Conductors: Class 2 stranded copper conductor, round or sector shaped. Class 5 stranded conductors can be offered upon request.

- Insulation: XLPE.

- Filler (optional): Halogen free filling compound.

- Outer Sheath: LSOH (SHF1). SHF2 can be offered upon request.

Core Identification

Two cores: Blue, Brown.

Three cores: Brown, Black, Grey. Four cores: Blue, Brown, Black, Grey.

Five cores: Blue, Brown, Black, Grey, Black. Multi cores: White with black numbers.  With yellow/green (optional)

Two cores + earth (3G): Yellow/green, Blue, Brown.

Three cores + earth (4G): Yellow/green, Brown, Black, Grey. Four cores + earth (5G): Yellow/green, Blue, Brown, Black, Grey.

www.addison-cables.com

ADDISON	13

IEC Standard Caledonian Offshore & Marine Cables

MariTox Marine Flame Retardant Power & Control Cables

www.caledonian-cables.co.uk

Mechanical and Thermal Properties

Bending Radius for Fixed Installations: 6×OD (OD>25mm); 4×OD (OD ≤25mm) Temperature Range: -30℃ ~ +80℃

Dimensions and Weight

MTX400 1RZ1-R Multicore 0.6/1kV (-R stands for class 2 conductor. For class 5 conductor, please change –R to –F)

| Part No. | Construction No. of cores×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MTX400-1RZ1-R-2C1.5 | 2×1.5 | 0.7 | 1.1 | 8.4 | 80 |
| MTX400-1RZ1-R-2C2.5 | 2×2.5 | 0.7 | 1.1 | 9.2 | 100 |
| MTX400-1RZ1-R-2C4 | 2×4 | 0.9 | 1.1 | 11.1 | 135 |
| MTX400-1RZ1-R-2C6 | 2×6 | 0.9 | 1.2 | 12.4 | 185 |
| MTX400-1RZ1-R-2C10 | 2×10 | 0.9 | 1.2 | 14.1 | 270 |
| MTX400-1RZ1-R-2C16 | 2×16 | 0.9 | 1.3 | 16.4 | 400 |
| MTX400-1RZ1-R-2C25 | 2×25 | 0.9 | 1.3 | 18.8 | 700 |
| MTX400-1RZ1-R-2C35 | 2×35 | 0.9 | 1.3 | 21.4 | 930 |
| MTX400-1RZ1-R-2C50 | 2×50 | 1.0 | 1.3 | 24.2 | 1290 |
| MTX400-1RZ1-R-3C1.5(3G1.5) | 3×(G)1.5 | 0.7 | 1.1 | 8.8 | 100 |
| MTX400-1RZ1-R-3C2.5(3G2.5) | 3×(G)2.5 | 0.7 | 1.1 | 9.8 | 130 |
| MTX400-1RZ1-R-3C4(3G4) | 3×(G)4 | 0.9 | 1.2 | 12.0 | 190 |
| MTX400-1RZ1-R-3C6(3G6) | 3×(G)6 | 0.9 | 1.2 | 13.2 | 250 |
| MTX400-1RZ1-R-3C10 | 3×10 | 0.9 | 1.3 | 15.2 | 380 |
| MTX400-1RZ1-R-3C16(3G16) | 3×16 | 0.9 | 1.3 | 17.5 | 560 |
| MTX400-1RZ1-R-3C25 | 3×25 | 0.9 | 1.5 | 20.7 | 875 |
| MTX400-1RZ1-R-3C35 | 3×35 | 0.9 | 1.6 | 23.5 | 1220 |
| MTX400-1RZ1-R-3C35S | 3×35 (sector shaped) | 0.9 | 1.5 | 20.1 | 1135 |
| MTX400-1RZ1-R-3C50 | 3×50 | 1.0 | 1.7 | 26.7 | 1780 |
| MTX400-1RZ1-R-3C50S | 3×50 (sector shaped) | 1.0 | 1.7 | 22.8 | 1530 |
| MTX400-1RZ1-R-3C70S | 3×70 (sector shaped) | 1.1 | 1.8 | 26.7 | 2150 |
| MTX400-1RZ1-R-3C95S | 3×95 (sector shaped) | 1.1 | 1.9 | 30.2 | 2900 |
| MTX400-1RZ1-R-3C120S | 3×120 (sector shaped) | 1.2 | 2.1 | 34.0 | 3675 |
| MTX400-1RZ1-R-4C1.5(4G1.5) | 4×(G)1.5 | 0.7 | 1.1 | 9.6 | 120 |
| MTX400-1RZ1-R-4C2.5(4G2.5) | 4×(G)2.5 | 0.7 | 1.1 | 10.7 | 165 |
| MTX400-1RZ1-R-4C4(4G4) | 4×(G)4 | 0.9 | 1.2 | 13.2 | 240 |
| MTX400-1RZ1-R-4C6(4G6) | 4×(G)6 | 0.9 | 1.2 | 14.5 | 320 |
| MTX400-1RZ1-R-4C10(4G10) | 4×(G)10 | 0.9 | 1.3 | 16.7 | 490 |

14	ADDISON	www.addison-cables.com

IEC Standard Caledonian Offshore & Marine Cables

MariTox Marine Flame Retardant Power & Control Cables

www.caledonian-cables.co.uk

| Part No. | Construction No. of cores×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MTX400-1RZ1-R-4C16(4G16) | 4×(G)16 | 0.9 | 1.4 | 19.5 | 740 |
| MTX400-1RZ1-R-4C25(4G25) | 4×(G)25 | 0.9 | 1.5 | 22.8 | 1145 |
| MTX400-1RZ1-R-4G35 | 4G35 | 0.9 | 1.7 | 26.0 | 1515 |
| MTX400-1RZ1-R-4G50 | 4G50 | 1.0 | 1.8 | 29.7 | 2340 |
| MTX400-1RZ1-R-5C1.5(5G1.5) | 5×(G)1.5 | 0.7 | 1.1 | 10.5 | 145 |
| MTX400-1RZ1-R-5C2.5(5G2.5) | 5×(G)2.5 | 0.7 | 1.2 | 11.9 | 205 |
| MTX400-1RZ1-R-5G6 | 5G6 | 0.9 | 1.3 | 16.1 | 400 |
| MTX400-1RZ1-R-5G16 | 5G16 | 0.9 | 1.5 | 21.6 | 920 |
| MTX400-1RZ1-R-6C1.5 | 6×1.5 | 0.7 | 1.2 | 11.6 | 180 |
| MTX400-1RZ1-R-7C1.5 | 7×1.5 | 0.7 | 1.2 | 11.7 | 195 |
| MTX400-1RZ1-R-8C1.5(8G1.5) | 8×(G)1.5 | 0.7 | 1.2 | 12.7 | 225 |
| MTX400-1RZ1-R-10C1.5 | 10×1.5 | 0.7 | 1.3 | 14.8 | 275 |
| MTX400-1RZ1-R-12C1.5 | 12×1.5 | 0.7 | 1.3 | 15.3 | 315 |
| MTX400-1RZ1-R-16C1.5 | 16×1.5 | 0.7 | 1.4 | 17.2 | 410 |
| MTX400-1RZ1-R-19C1.5 | 19×1.5 | 0.7 | 1.4 | 18.1 | 470 |
| MTX400-1RZ1-R-24C1.5 | 24×1.5 | 0.7 | 1.5 | 21.3 | 620 |
| MTX400-1RZ1-R-5C2.5 | 5×2.5 | 0.7 | 1.2 | 11.9 | 210 |
| MTX400-1RZ1-R-7C2.5 | 7×2.5 | 0.7 | 1.2 | 13.2 | 280 |
| MTX400-1RZ1-R-12C2.5 | 12×2.5 | 0.7 | 1.3 | 17.4 | 460 |
| MTX400-1RZ1-R-19C2.5 | 19×2.5 | 0.7 | 1.4 | 20.6 | 690 |
| MTX400-1RZ1-R-24C2.5 | 24×2.5 | 0.7 | 1.5 | 24.3 | 880 |
| MTX400-1RZ1-R-27C2.5 | 27×2.5 | 0.7 | 1.5 | 24.6 | 970 |
| MTX400-1RZ1-R-37C2.5 | 37×2.5 | 0.7 | 1.6 | 27.7 | 1300 |

www.addison-cables.com

ADDISON	15