IEC Standard Caledonian Offshore & Marine Cables

MariTox Marine Flame Retardant Power & Control Cables

www.caledonian-cables.co.uk

MTX300 0.6/1 kV HEPR Insulated, LSOH (SHF1) Sheathed Flame Retardant Power & Control Cables (Single Core)

Application

These cables are used for fixed installations on ships and offshore units in all locations. These cables are flame retardant, low smoke & halogen free.

Standards

	DIN 89160/98

	IEC 60092-353

	IEC 60332-1

	IEC 60332-3-22

	IEC 60754-1/2

	IEC 61034

Stranded Copper Conductor HEPR Insulation

LSOH (SHF1) Sheath

Construction

- Conductors: Class 2 stranded copper conductor.

- Insulation: HEPR.

- Outer Sheath: LSOH (SHF1).

Core Identification

Single core: Natural colour (beige).

Mechanical and Thermal Properties

Bending Radius for Fixed Installations: 6×OD (OD>25mm); 4×OD (OD ≤25mm) Temperature Range: -20℃ ~ +75℃

www.addison-cables.com

ADDISON	21

IEC Standard Caledonian Offshore & Marine Cables

MariTox Marine Flame Retardant Power & Control Cables

www.caledonian-cables.co.uk

Dimensions and Weight

| Part No. | Construction No. of cores×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MTX300-1G7Z1-R-1C4 | 1×4 | 0.7 | 1.2 | 6.5 | 80 |
| MTX300-1G7Z1-R-1C6 | 1×6 | 0.7 | 1.2 | 7.5 | 110 |
| MTX300-1G7Z1-R-1C10 | 1×10 | 0.7 | 1.2 | 8.5 | 150 |
| MTX300-1G7Z1-R-1C16 | 1×16 | 0.7 | 1.2 | 9.5 | 220 |
| MTX300-1G7Z1-R-1C25 | 1×25 | 0.9 | 1.2 | 11.0 | 320 |
| MTX300-1G7Z1-R-1C35 | 1×35 | 0.9 | 1.2 | 12.0 | 420 |
| MTX300-1G7Z1-R-1C50 | 1×50 | 1.0 | 1.3 | 13.5 | 560 |
| MTX300-1G7Z1-R-1C70 | 1×70 | 1.1 | 1.3 | 15.5 | 780 |
| MTX300-1G7Z1-R-1C95 | 1×95 | 1.1 | 1.4 | 17.8 | 1030 |
| MTX300-1G7Z1-R-1C120 | 1×120 | 1.2 | 1.4 | 19.3 | 1290 |
| MTX300-1G7Z1-R-1C150 | 1×150 | 1.4 | 1.5 | 21.3 | 1590 |
| MTX300-1G7Z1-R-1C185 | 1×185 | 1.6 | 1.5 | 23.5 | 1960 |
| MTX300-1G7Z1-R-1C240 | 1×240 | 1.7 | 1.6 | 26.5 | 2560 |
| MTX300-1G7Z1-R-1C300 | 1×300 | 1.8 | 1.7 | 29.5 | 3200 |

22	ADDISON	www.addison-cables.com