BS 6883&BS 7917 Caledonian Offshore & Marine Cables

Flame Retardant Instrumentation & Control Cables

www.caledonian-cables.co.uk

150/250V HF-EPR Insulated, SW2/SW4 Sheathed, Collectively Screened Armoured Flame Retardant Instrumentation & Control Cables

Application

These elastomeric insulated cables are designed for fixed wiring in ships and on mobile offshore units, suitable for use in instrumentation, lighting and control circuits.

Standards

	BS 6883

- IEC 60332-3A Flame retardant

	IEC 60754-1; IEC 60754-2

Corrosivity

- IEC 61034-2 Smoke density

- Cold bend and impact (-40°C) (on request)

- CSA C22.2 No. 38-95 (on request)

Construction

Stranded Tinned Copper Conductor HF-EPR GP4 Insulation

Aluminium/Polyester Tape + Drain Wire SW2/SW4 Inner Sheath

Galvanized Steel Wire Braid SW2/SW4 Outer Sheath

- Conductor: Tinned copper wire stranded circular cl. 2 BS 6360/IEC 60228.

- Insulation: HF-EPR GP4 according to BS 7655 1.2.

- Lay-up: Pairs, triples.

- Collective Screen: Aluminium/polyester tape + drain wire tinned copper.

- Inner Sheath: Halogen free thermosetting compound SW4 according to BS 7655 2.6 or reduced halogen thermosetting compound SW2 according to BS 7655 2.6.

- Armour: Galvanized steel wire braid. Tinned bronze wire braid can be offered upon request.

- Outer Sheath: Halogen free thermosetting compound SW4 according to BS 7655 2.6 or reduced halogen thermosetting compound SW2 according to BS 7655 2.6.

36	ADDISON	www.addison-cables.com

BS 6883&BS 7917 Caledonian Offshore & Marine Cables

Flame Retardant Instrumentation & Control Cables

www.caledonian-cables.co.uk

Mechanical and Thermal Properties

Minimum Internal Bending Radius: 8×OD Temperature Range: -40℃ ~ +90℃

Dimensions and Weight

| Construction No. of cores×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Inner Sheath Thickness mm | Minimum Diameter Over Inner Sheath mm | Maximum Diameter Over Inner Sheath mm | Nominal Armour Wire Diameter mm | Nominal Outer Sheath Thickness mm | Minimum Overall Diameter mm | Maximum Overall Diameter mm | Approx. Weight kg/km |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Multipair |  |  |  |  |  |  |  |  |  |
| 3×2×0.75 | 0.8 | 1.2 | 12.6 | 14.5 | 0.3 | 1.4 | 16.7 | 19.0 | 390 |
| 7×2×0.75 | 0.8 | 1.4 | 16.6 | 18.7 | 0.3 | 1.5 | 20.9 | 23.8 | 620 |
| 12×2×0.75 | 0.8 | 1.6 | 21.7 | 24.2 | 0.3 | 1.7 | 26.4 | 29.5 | 930 |
| 20×2×0.75 | 0.8 | 1.8 | 27.3 | 30.1 | 0.45 | 2.0 | 33.3 | 37.1 | 1460 |
| 27×2×0.75 | 0.8 | 1.9 | 31.1 | 34.2 | 0.45 | 2.2 | 37.4 | 41.4 | 1810 |
| 37×2×0.75 | 0.8 | 2.1 | 34.4 | 37.7 | 0.45 | 2.3 | 41.0 | 45.5 | 2270 |
| 3×2×1 | 0.8 | 1.2 | 13.3 | 15.3 | 0.3 | 1.4 | 17.4 | 19.8 | 410 |
| 7×2×1 | 0.8 | 1.4 | 17.6 | 19.8 | 0.3 | 1.6 | 22.1 | 25.1 | 680 |
| 12×2×1 | 0.8 | 1.6 | 23.1 | 25.7 | 0.3 | 1.8 | 28.0 | 31.2 | 1010 |
| 20×2×1 | 0.8 | 1.8 | 29.0 | 31.9 | 0.45 | 2.1 | 35.3 | 39.2 | 1600 |
| 27×2×1 | 0.8 | 2.0 | 33.3 | 36.6 | 0.45 | 2.2 | 39.7 | 44.2 | 2000 |
| 37×2×1 | 0.8 | 2.2 | 36.9 | 40.3 | 0.45 | 2.4 | 43.7 | 48.3 | 2540 |
| Multitriple |  |  |  |  |  |  |  |  |  |
| 3×3×0.75 | 0.8 | 1.3 | 14.2 | 16.2 | 0.3 | 1.4 | 18.3 | 20.7 | 480 |
| 7×3×0.75 | 0.8 | 1.4 | 19.4 | 21.9 | 0.3 | 1.6 | 24.0 | 27.0 | 780 |
| 12×3×0.75 | 0.8 | 1.7 | 24.2 | 26.8 | 0.45 | 1.9 | 29.3 | 32.9 | 1320 |
| 3×3×1 | 0.8 | 1.3 | 15.1 | 17.1 | 0.3 | 1.5 | 19.4 | 22.2 | 530 |
| 7×3×1 | 0.8 | 1.5 | 20.9 | 23.4 | 0.3 | 1.7 | 25.6 | 28.7 | 890 |
| 12×3×1 | 0.8 | 1.7 | 25.8 | 28.5 | 0.45 | 2.0 | 31.8 | 35.5 | 1480 |

www.addison-cables.com

ADDISON	37