BS 6883&BS 7917 Caledonian Offshore & Marine Cables

MV Flame Retardant Power & Control Cables

www.caledonian-cables.co.uk

  - /6.6kV, 6.35/11kV, 8.7/15kV HF-EPR Insulated, SW2/SW4

Sheathed Unarmoured Flame Retardant Power & Control Cables (Radial Field)

Application

These medium voltage elastomeric insulated cables are designed for ﬁxed wiring in ships and on mobile offshore units, suitable for use in power and control applications.

Standards

	BS 6883

    - IEC 60332-3A Flame retardant

	IEC 60754-1; IEC 60754-2

Corrosivity

    - IEC 61034-2 Smoke density

    - Cold bend and impact (-40°C) (on request)

    - CSA C22.2 No. 38-95 (on request)

Construction

Stranded Tinned Copper Conductor Conductor Screen

HF-EPR GP5 Insulation Insulation Screen SW2/SW4 Outer Sheath

    - Conductor: Tinned copper wire stranded circular cl. 2 BS 6360/IEC 60228.

    - Conductor Screen: Semiconducting layer or tape.

    - Insulation: HF-EPR GP5 according to BS 7655 1.2.

    - Insulation Screen: Semiconducting layer or tape +Tinned copper tape.

    - Outer Sheath: Halogen free thermosetting compound SW4 according to BS 7655 2.6 or reduced halogen thermosetting compound SW2 according to BS 7655 2.6.

Mechanical and Thermal Properties

Minimum Internal Bending Radius: 15×OD (single core); 20×OD (three core) Temperature Range: -40℃ ~ +90℃

6	ADDISON	www.addison-cables.com

BS 6883&BS 7917 Caledonian Offshore & Marine Cables

MV Flame Retardant Power & Control Cables

www.caledonian-cables.co.uk

Dimensions and Weight

3.8/6.6kV

| Construction No. of cores×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Outer Sheath Thickness mm | Minimum Overall Diameter mm | Maximum Overall Diameter mm | Approx. Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| 1×16 | 3.0 | 1.3 | 16.0 | 18.0 | 492 |
| 1×25 | 3.0 | 1.3 | 17.6 | 19.7 | 658 |
| 1×35 | 3.0 | 1.4 | 18.7 | 20.8 | 776 |
| 1×50 | 3.0 | 1.4 | 19.9 | 22.3 | 942 |
| 1×70 | 3.0 | 1.5 | 21.8 | 24.3 | 1229 |
| 1×95 | 3.0 | 1.6 | 23.7 | 26.3 | 1546 |
| 1×120 | 3.0 | 1.6 | 25.4 | 28.0 | 1890 |
| 1×150 | 3.0 | 1.7 | 27.0 | 29.8 | 2242 |
| 1×185 | 3.0 | 1.8 | 29.0 | 32.1 | 2713 |
| 1×240 | 3.0 | 1.9 | 31.7 | 35.0 | 3427 |
| 1×300 | 3.0 | 2.0 | 34.3 | 37.6 | 4177 |
| 1×400 | 3.0 | 2.1 | 37.6 | 41.1 | 5145 |
| 1×500 | 3.2 | 2.3 | 41.4 | 45.5 | 6408 |
| 1×630 | 3.2 | 2.4 | 45.1 | 49.2 | 8134 |
| 3×16 | 3.0 | 1.8 | 32.7 | 36.0 | 1482 |
| 3×25 | 3.0 | 2.0 | 36.5 | 39.9 | 2031 |
| 3×35 | 3.0 | 2.0 | 38.4 | 41.9 | 2359 |
| 3×50 | 3.0 | 2.2 | 41.3 | 45.3 | 2918 |
| 3×70 | 3.0 | 2.3 | 45.3 | 49.4 | 3788 |
| 3×95 | 3.0 | 2.5 | 49.3 | 53.9 | 4776 |
| 3×120 | 3.0 | 2.6 | 53.1 | 57.8 | 5868 |
| 3×150 | 3.0 | 2.7 | 56.5 | 61.4 | 6933 |
| 3×185 | 3.0 | 2.9 | 60.8 | 66.1 | 8401 |
| 3×240 | 3.0 | 3.1 | 66.6 | 72.2 | 10616 |

6.35/11kV

| Construction No. of cores×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Outer Sheath Thickness mm | Minimum Overall Diameter mm | Maximum Overall Diameter mm | Approx. Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| 1×16 | 3.4 | 1.3 | 16.8 | 18.8 | 524 |
| 1×25 | 3.4 | 1.4 | 18.6 | 20.7 | 704 |
| 1×35 | 3.4 | 1.4 | 19.4 | 21.9 | 813 |
| 1×50 | 3.4 | 1.5 | 20.8 | 23.3 | 994 |
| 1×70 | 3.4 | 1.5 | 22.6 | 25.1 | 1272 |
| 1×95 | 3.4 | 1.6 | 24.4 | 27.1 | 1592 |
| 1×120 | 3.4 | 1.7 | 26.3 | 29.0 | 1956 |
| 1×150 | 3.4 | 1.7 | 27.8 | 30.6 | 2294 |
| 1×185 | 3.4 | 1.8 | 29.8 | 32.9 | 2769 |
| 1×240 | 3.4 | 1.9 | 32.5 | 35.8 | 3487 |

www.addison-cables.com

ADDISON	7

BS 6883&BS 7917 Caledonian Offshore & Marine Cables

MV Flame Retardant Power & Control Cables

www.caledonian-cables.co.uk

| Construction No. of cores×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Outer Sheath Thickness mm | Minimum Overall Diameter mm | Maximum Overall Diameter mm | Approx. Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| 1×300 | 3.4 | 2.0 | 35.0 | 38.4 | 4242 |
| 1×400 | 3.4 | 2.1 | 38.4 | 41.9 | 5208 |
| 1×500 | 3.4 | 2.3 | 41.8 | 45.8 | 6442 |
| 1×630 | 3.4 | 2.4 | 45.5 | 49.6 | 8176 |
| 3×16 | 3.4 | 1.9 | 34.5 | 37.9 | 1601 |
| 3×25 | 3.4 | 2.0 | 38.2 | 41.6 | 2139 |
| 3×35 | 3.4 | 2.1 | 40.2 | 44.1 | 2497 |
| 3×50 | 3.4 | 2.2 | 43.0 | 47.0 | 3040 |
| 3×70 | 3.4 | 2.4 | 47.1 | 51.3 | 3949 |
| 3×95 | 3.4 | 2.5 | 51.0 | 55.6 | 4919 |
| 3×120 | 3.4 | 2.7 | 55.0 | 59.8 | 6055 |
| 3×150 | 3.4 | 2.8 | 58.4 | 63.3 | 7132 |
| 3×185 | 3.4 | 3.0 | 62.7 | 68.1 | 8613 |
| 3×240 | 3.4 | 3.2 | 68.5 | 74.1 | 10848 |

8.7/15kV

| Construction No. of cores×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Outer Sheath Thickness mm | Minimum Overall Diameter mm | Maximum Overall Diameter Mm | Approx. Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| 1×25 | 4.5 | 1.5 | 20.9 | 23.4 | 808 |
| 1×35 | 4.5 | 1.5 | 21.7 | 24.3 | 921 |
| 1×50 | 4.5 | 1.5 | 22.9 | 25.5 | 1110 |
| 1×70 | 4.5 | 1.6 | 24.9 | 27.5 | 1396 |
| 1×95 | 4.5 | 1.7 | 26.7 | 29.5 | 1726 |
| 1×120 | 4.5 | 1.8 | 28.6 | 31.4 | 2099 |
| 1×150 | 4.5 | 1.8 | 30.1 | 33.3 | 2445 |
| 1×185 | 4.5 | 1.9 | 32.1 | 35.3 | 2929 |
| 1×240 | 4.5 | 2.0 | 34.8 | 38.2 | 3661 |
| 1×300 | 4.5 | 2.1 | 37.3 | 40.8 | 4429 |
| 1×400 | 4.5 | 2.2 | 40.7 | 44.6 | 5390 |
| 1×500 | 4.5 | 2.4 | 44.1 | 48.2 | 6638 |
| 1×630 | 4.5 | 2.5 | 47.8 | 52.0 | 8415 |
| 3×25 | 4.5 | 2.2 | 43.1 | 47.1 | 2458 |
| 3×35 | 4.5 | 2.3 | 45.2 | 49.2 | 2832 |
| 3×50 | 4.5 | 2.4 | 47.9 | 52.1 | 3395 |
| 3×70 | 4.5 | 2.6 | 52.1 | 56.7 | 4336 |
| 3×95 | 4.5 | 2.7 | 55.9 | 60.7 | 5334 |
| 3×120 | 4.5 | 2.9 | 59.9 | 64.9 | 6500 |
| 3×150 | 4.5 | 3.0 | 63.3 | 68.7 | 7602 |
| 3×185 | 4.5 | 3.2 | 67.6 | 73.2 | 9116 |

8	ADDISON	www.addison-cables.com