ADDISON

Flame Retardant RG59 B/U CWB/SWB/SWA Armoured Coaxial cables

LSZH Outer Sheath

Tinned Copper Braid

Aluminium+polyester/Aluminium Tape

PE

Solid Bare Copper

LSZH Inner Sheath

Tinned Copper Drain Wire

Braid or Wire Armoured

Application

These 75Ω coaxial cables are suitable for installation on board of ships and other indoor marine environments.

STANDARDS

Basic design adapted to MIL-C-17

FIRE PERFORMANCE

Flame Retardance (Single Vertical EN 60332-1-2; IEC 60332-1-2; BS EN 60332-1-2; VDE Wire Test) 0482-332-1 ; NBN C 30-004 (cat. F1); NF C32-070-2.1(C2);

CEI 20-35/1-2; EN 50265-2-1*; DIN VDE 0482-265-2-1*

| Reduced Fire Propagation | EN 60332-3-24 (cat. C); IEC 60332-3-24; BS EN 60332-3-24; |  |
| --- | --- | --- |
| (Vertically-mounted bundled wires VDE 0482-332-3; NBN C 30-004 (cat. F2); NF C32-070-2.2(C1); |  |  |
| & cable test) | CEI 20-22/3-4; EN 50266-2-4*; DIN VDE 0482-266-2-4 |  |
| Halogen Free | IEC 60754-1; EN 50267-2-1; DIN VDE 0482-267-2-1; |  |
|  | CEI 20-37/2-1 ; BS 6425-1* |  |
| No Corrosive Gas Emission | IEC 60754-2; EN 50267-2-2; DIN VDE 0482-267-2-2; |  |
|  | CEI 20-37/2-2 ; BS 6425-2* |  |
| Minimum Smoke Emission | IEC 61034-1&2; EN 61034 -1&2; DIN VDE 0482-1034-1&2; |  |
|  | CEI 20-37/3-1&2; EN 50268-1&2*; BS 7622-1&2* |  |
| No Toxic gases | NES 02-713; NF C 20-454 |  |

Note: Asterisk * denotes superseded standard.

CABLE CONSTRUCTION

Conductors: 20AWG solid bare copper.

Insulation: PE compound.

Screen1: Aluminium/polyester or aluminium tape.

Screen2: Tinned copper braid.

126	Caledonian

Caledonian

Flame Retardant Coaxial Cables

www.caledonian-cables.co.uk	www.addison-cables.com

Inner Sheath: Low smoke and halogen-free polyolefin, coloured black.

Armouring:

cwb: copper Wire Braid swb: Steel Wire Braid swa: Steel Wire Armour

Outer Sheath: Thermoplastic LSZH compound type LTS3 as per BS 7655-6.1 (Thermosetting LSZH compound type SW2-SW4 as per BS 7655-2.6 can be offered.) . UV resistance, hydrocarbon resistance, oil resistance, anti rodent and anti termite properties can be offered as option.

Physical AND THERMAL PROPERTIES

Temperature Range: -30°C - +75°C

Minimum Bending Radius: 15 X Overall Diameter

Electrical Properties

| AWG |  | 20 |
| --- | --- | --- |
| Nominal Conductor Diameter | mm | 0.58 |
| Impedance | Ω | 75+/-5 |
| Nominal Attenuation@100MHz | dB/100m | 7.6 |
| Nominal Attenuation@270MHz | dB/100m | 12.5 |
| Nominal Attenuation@540MHz | dB/100m | 17.9 |
| Nominal Attenuation@720MHz | dB/100m | 20.9 |
| Nominal Attenuation@750MHz | dB/100m | 21.3 |
| Nominal Attenuation@1000MHz | dB/100m | 24.9 |
| Capacitance | pF/m | 53.5 |
| Velocity of Propagation | % | 83 |
| Conductor DCR | Ω/km | 32.8 |
| Shield DCR | Ω/km | 12.5 |
| Inductance | μH/m | 0.318 |
| Time Delay | ns/m | 4.0 |

ADDISON   127

ADDISON

CONSTRUCTION PARAMETERS

|  |  | Nominal Inner |  | Nominal |  | Nominal |  |  | Nominal | Nominal |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cable Code |  | Conductor |  | Insulation |  | Sheath |  |  | Overall |  |  |
|  |  |  |  |  |  |  |  |  |  | Weight |  |
|  |  | Diameter |  | Thickness |  | Thickness |  |  | Diameter |  |  |
|  |  | mm |  | mm |  | mm |  |  | mm | kg/km |  |
| FTX-RG59 CWB |  | 0.58 |  | 1.4 |  | 1.2 |  |  | 9.78 | 146 |  |
| FTX-RG59 SWB |  | 0.58 |  | 1.4 |  | 1.2 |  |  | 9.78 | 114 |  |
| FTX-RG59 SWA |  | 0.58 |  | 1.4 |  | 1.2 |  |  | 10.8 | 220 |  |
| 300/500V | NMIL-C-17 |  | Flame Retardancy |  | Reduced Fire Propagation |  |  |  |  |  |  |
|  |  |  |  |  | NF C32-070-2.2(C1) |  |  |  |  |  |  |
| Rated Voltage |  |  | NF C32-070-2.1(C2) |  | IEC60332-3-24 |  |  |  |  |  |  |
|  | Standard |  | IEC60332-1-2/EN50265-2-1 |  | EN50266-2-4 |  |  |  |  |  |  |
|  |  |  |  |  | Zero |  |  |  |  |  |  |
|  | Low Corrosivity |  | Low Smoke Emission |  | Halogen Free |  |  |  |  |  |  |
|  | IEC60754-2 |  |  |  |  |  |  |  |  |  |  |
| Low Toxicity |  |  | IEC 61034-1&2 |  | IEC60754-1 |  |  |  |  |  |  |
|  | EN50267-2-2/3 |  |  |  |  |  |  |  |  |  |  |
| NES 02-713/NF C 20-454 | NF C 32-074 |  | EN 50268-1&2/NF C32-073 |  | EN50267-2-1 |  |  |  |  |  |  |

128	Caledonian