MRE-M2X(St)H 150/250V Mica Tape + XLPE Insulated, LSOH (SHF1) Sheathed, Overall Screened Fire Resistant Instrumentation

& Control Cables (Multipair/Multitriple)

Application

These cables are used on board of ships in all locations for fixed installations not subject to mechanical risk complying with IEC standards 60092-352 in safety circuit, where fire resistance is required. These cables are fire resistant, flame retardant, low smoke & halogen free, suitable for installations on passenger ships, as on other commercial vessels.

Standards

	IEC 60092-350/351/376/359

	IEC 60331-21

	IEC 60332-1

	IEC 60332-3-22

	IEC 60754-1/2

	IEC 61034

Stranded Copper Conductor Mica Tape + XLPE Insulation Al/polyester Tape + Drain Wire LSOH (SHF1) Outer Sheath

Construction

- Conductors: Class 2 stranded copper conductor.

- Insulation: Mica tape + XLPE.

- Cabling Element: Pair/Triple.

- Overall Screen: Al/polyester tape.

- Drain Wire: Tinned copper wire.

- Outer Sheath: LSOH (SHF1). SHF2 can be offered upon request.

Core Identification

Pair: White/blue with printed pair number and core number. Triple: White/blue/red with printed triple number.

Mechanical and Thermal Properties

Bending Radius for Fixed Installations: 6×OD (OD>25mm); 4×OD (OD ≤25mm) Temperature Range: -30℃ ~ +80℃

Dimensions and Weight

| Part No. | Construction No. of elements×No. of cores in element×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MRE-M2X(St)H-1P0.75 | 1×2×0.75 | 0.5 | 1.0 | 8.1 | 70 |
| MRE-M2X(St)H-2P0.75 | 2×2×0.75* | 0.5 | 1.1 | 9.5 | 110 |
| MRE-M2X(St)H-3P0.75 | 3×2×0.75 | 0.5 | 1.2 | 13.3 | 170 |
| MRE-M2X(St)H-4P0.75 | 4×2×0.75 | 0.5 | 1.3 | 14.3 | 210 |
| MRE-M2X(St)H-7P0.75 | 7×2×0.75 | 0.5 | 1.4 | 17.3 | 320 |
| MRE-M2X(St)H-8P0.75 | 8×2×0.75 | 0.5 | 1.4 | 18.4 | 360 |
| MRE-M2X(St)H-10P0.75 | 10×2×0.75 | 0.5 | 1.5 | 20.9 | 430 |
| MRE-M2X(St)H-12P07.5 | 12×2×0.75 | 0.5 | 1.5 | 21.7 | 490 |
| MRE-M2X(St)H-14P0.75 | 14×2×0.75 | 0.5 | 1.6 | 22.7 | 560 |
| MRE-M2X(St)H-16P0.75 | 16×2×0.75 | 0.5 | 1.6 | 24.4 | 630 |
| MRE-M2X(St)H-19P0.75 | 19×2×0.75 | 0.5 | 1.7 | 25.7 | 730 |
| MRE-M2X(St)H-24P0.75 | 24×2×0.75 | 0.5 | 1.8 | 29.3 | 910 |
| MRE-M2X(St)H-30P0.75 | 30×2×0.75 | 0.5 | 2.0 | 33.1 | 1140 |
| MRE-M2X(St)H-32P0.75 | 32×2×0.75 | 0.5 | 2.0 | 33.6 | 1190 |
| MRE-M2X(St)H-37P0.75 | 37×2×0.75 | 0.5 | 2.0 | 35.3 | 1340 |
| MRE-M2X(St)H-1P1.0 | 1×2×1.0 | 0.5 | 1.1 | 8.7 | 90 |
| MRE-M2X(St)H-2P1.0 | 2×2×1.0* | 0.5 | 1.1 | 9.9 | 130 |
| MRE-M2X(St)H-3P1.0 | 3×2×1.0 | 0.5 | 1.3 | 14.2 | 200 |
| MRE-M2X(St)H-4P1.0 | 4×2×1.0 | 0.5 | 1.3 | 15.1 | 240 |
| MRE-M2X(St)H-7P1.0 | 7×2×1.0 | 0.5 | 1.4 | 18.3 | 370 |
| MRE-M2X(St)H-8P1.0 | 8×2×1.0 | 0.5 | 1.5 | 19.7 | 430 |
| MRE-M2X(St)H-10P1.0 | 10×2×1.0 | 0.5 | 1.6 | 22.3 | 520 |
| MRE-M2X(St)H-12P1.0 | 12×2×1.0 | 0.5 | 1.6 | 23.2 | 590 |
| MRE-M2X(St)H-14P1.0 | 14×2×1.0 | 0.5 | 1.6 | 24.1 | 660 |
| MRE-M2X(St)H-16P1.0 | 16×2×1.0 | 0.5 | 1.7 | 26.1 | 760 |
| MRE-M2X(St)H-19P1.0 | 19×2×1.0 | 0.5 | 1.7 | 27.3 | 860 |
| MRE-M2X(St)H-24P1.0 | 24×2×1.0 | 0.5 | 1.9 | 31.3 | 1100 |
| MRE-M2X(St)H-30P1.0 | 30×2×1.0 | 0.5 | 2.0 | 35.1 | 1350 |

| Part No. | Construction No. of elements×No. of cores in element×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MRE-M2X(St)H-32P1.0 | 32×2×1.0 | 0.5 | 2.1 | 35.9 | 1440 |
| MRE-M2X(St)H-37P1.0 | 37×2×1.0 | 0.5 | 2.1 | 37.7 | 1620 |
| MRE-M2X(St)H-1P1.5 | 1×2×1.5 | 0.6 | 1.1 | 9.5 | 100 |
| MRE-M2X(St)H-2P1.5 | 2×2×1.5* | 0.6 | 1.1 | 10.9 | 160 |
| MRE-M2X(St)H-3P1.5 | 3×2×1.5 | 0.6 | 1.3 | 15.7 | 250 |
| MRE-M2X(St)H-4P1.5 | 4×2×1.5 | 0.6 | 1.4 | 16.9 | 310 |
| MRE-M2X(St)H-7P1.5 | 7×2×1.5 | 0.6 | 1.5 | 20.5 | 490 |
| MRE-M2X(St)H-8P1.5 | 8×2×1.5 | 0.6 | 1.5 | 21.9 | 550 |
| MRE-M2X(St)H-10P1.5 | 10×2×1.5 | 0.6 | 1.7 | 25.0 | 670 |
| MRE-M2X(St)H-12P1.5 | 12×2×1.5 | 0.6 | 1.7 | 26.0 | 770 |
| MRE-M2X(St)H-14P1.5 | 14×2×1.5 | 0.6 | 1.7 | 27.0 | 870 |
| MRE-M2X(St)H-16P1.5 | 16×2×1.5 | 0.6 | 1.8 | 29.3 | 990 |
| MRE-M2X(St)H-19P1.5 | 19×2×1.5 | 0.6 | 1.9 | 30.8 | 1150 |
| MRE-M2X(St)H-24P1.5 | 24×2×1.5 | 0.6 | 2.0 | 35.1 | 1440 |
| MRE-M2X(St)H-30P1.5 | 30×2×1.5 | 0.6 | 2.2 | 39.6 | 1790 |
| MRE-M2X(St)H-32P1.5 | 32×2×1.5 | 0.6 | 2.2 | 40.3 | 1890 |
| MRE-M2X(St)H-37P1.5 | 37×2×1.5 | 0.6 | 2.3 | 42.5 | 2160 |
| MRE-M2X(St)H-1T0.75 | 1×3×0.75 | 0.5 | 1.1 | 8.7 | 90 |
| MRE-M2X(St)H-2T0.75 | 2×3×0.75 | 0.5 | 1.2 | 13.5 | 180 |
| MRE-M2X(St)H-3T0.75 | 3×3×0.75 | 0.5 | 1.3 | 14.5 | 230 |
| MRE-M2X(St)H-4T0.75 | 4×3×0.75 | 0.5 | 1.3 | 15.9 | 280 |
| MRE-M2X(St)H-7T0.75 | 7×3×0.75 | 0.5 | 1.5 | 20.2 | 460 |
| MRE-M2X(St)H-8T0.75 | 8×3×0.75 | 0.5 | 1.5 | 21.6 | 510 |
| MRE-M2X(St)H-10T0.75 | 10×3×0.75 | 0.5 | 1.6 | 24.6 | 620 |
| MRE-M2X(St)H-12T07.5 | 12×3×0.75 | 0.5 | 1.7 | 26.2 | 720 |
| MRE-M2X(St)H-14T0.75 | 14×3×0.75 | 0.5 | 1.7 | 27.3 | 810 |
| MRE-M2X(St)H-16T0.75 | 16×3×0.75 | 0.5 | 1.8 | 29.2 | 920 |
| MRE-M2X(St)H-19T0.75 | 19×3×0.75 | 0.5 | 1.9 | 31.6 | 1080 |
| MRE-M2X(St)H-24T0.75 | 24×3×0.75 | 0.5 | 2.0 | 35.1 | 1340 |
| MRE-M2X(St)H-30T0.75 | 30×3×0.75 | 0.5 | 2.2 | 39.1 | 1660 |
| MRE-M2X(St)H-32T0.75 | 32×3×0.75 | 0.5 | 2.2 | 40.5 | 1760 |
| MRE-M2X(St)H-37T0.75 | 37×3×0.75 | 0.5 | 2.3 | 42.7 | 2000 |
| MRE-M2X(St)H-1T1.0 | 1×3×1.0 | 0.5 | 1.1 | 9.2 | 110 |
| MRE-M2X(St)H-2T1.0 | 2×3×1.0 | 0.5 | 1.3 | 14.6 | 210 |
| MRE-M2X(St)H-3T1.0 | 3×3×1.0 | 0.5 | 1.3 | 15.5 | 270 |
| MRE-M2X(St)H-4T1.0 | 4×3×1.0 | 0.5 | 1.4 | 17.2 | 340 |

| Part No. | Construction No. of elements×No. of cores in element×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MRE-M2X(St)H-7T1.0 | 7×3×1.0 | 0.5 | 1.5 | 21.6 | 540 |
| MRE-M2X(St)H-8T1.0 | 8×3×1.0 | 0.5 | 1.6 | 23.3 | 620 |
| MRE-M2X(St)H-10T1.0 | 10×3×1.0 | 0.5 | 1.7 | 26.5 | 740 |
| MRE-M2X(St)H-12T1.0 | 12×3×1.0 | 0.5 | 1.8 | 28.2 | 870 |
| MRE-M2X(St)H-14T1.0 | 14×3×1.0 | 0.5 | 1.8 | 29.4 | 980 |
| MRE-M2X(St)H-16T1.0 | 16×3×1.0 | 0.5 | 1.9 | 31.4 | 1110 |
| MRE-M2X(St)H-19T1.0 | 19×3×1.0 | 0.5 | 2.0 | 34.1 | 1310 |
| MRE-M2X(St)H-24T1.0 | 24×3×1.0 | 0.5 | 2.1 | 37.9 | 1620 |
| MRE-M2X(St)H-30T1.0 | 30×3×1.0 | 0.5 | 2.3 | 42.2 | 2010 |
| MRE-M2X(St)H-32T1.0 | 32×3×1.0 | 0.5 | 2.4 | 43.9 | 2150 |
| MRE-M2X(St)H-37T1.0 | 37×3×1.0 | 0.5 | 2.4 | 46.0 | 2430 |
| MRE-M2X(St)H-1T1.5 | 1×3×1.5 | 0.6 | 1.1 | 10.0 | 130 |
| MRE-M2X(St)H-2T1.5 | 2×3×1.5 | 0.6 | 1.3 | 16.0 | 260 |
| MRE-M2X(St)H-3T1.5 | 3×3×1.5 | 0.6 | 1.4 | 17.2 | 340 |
| MRE-M2X(St)H-4T1.5 | 4×3×1.5 | 0.6 | 1.4 | 18.9 | 430 |
| MRE-M2X(St)H-7T1.5 | 7×3×1.5 | 0.6 | 1.6 | 24.0 | 700 |
| MRE-M2X(St)H-8T1.5 | 8×3×1.5 | 0.6 | 1.7 | 25.9 | 800 |
| MRE-M2X(St)H-10T1.5 | 10×3×1.5 | 0.6 | 1.8 | 29.5 | 970 |
| MRE-M2X(St)H-12T1.5 | 12×3×1.5 | 0.6 | 1.9 | 31.4 | 1130 |
| MRE-M2X(St)H-14T1.5 | 14×3×1.5 | 0.6 | 2.0 | 33.0 | 1300 |
| MRE-M2X(St)H-16T1.5 | 16×3×1.5 | 0.6 | 2.0 | 35.0 | 1460 |
| MRE-M2X(St)H-19T1.5 | 19×3×1.5 | 0.6 | 2.1 | 37.9 | 1710 |
| MRE-M2X(St)H-24T1.5 | 24×3×1.5 | 0.6 | 2.3 | 42.4 | 2140 |
| MRE-M2X(St)H-30T1.5 | 30×3×1.5 | 0.6 | 2.5 | 47.2 | 2660 |
| MRE-M2X(St)H-32T1.5 | 32×3×1.5 | 0.6 | 2.5 | 48.9 | 2820 |
| MRE-M2X(St)H-37T1.5 | 37×3×1.5 | 0.6 | 2.6 | 51.4 | 3210 |

*: 2 pairs are assembled as a quad.