IEC Standard Caledonian Offshore & Marine Cables

MariSig Fire Resistant Instrumentation & Control Cables

www.caledonian-cables.co.uk

MRE-M2XH PiMF/TiMF 150/250V Mica Tape + XLPE Insulated, LSOH (SHF1) Sheathed, Individual Screened Fire Resistant Instrumentation & Control Cables (Multipair/Multitriple)

Application

These cables are used on board of ships in all locations for fixed installations not subject to mechanical risk complying with IEC standards 60092-352 in safety circuit, where fire resistance is required. These cables are fire resistant, flame retardant, low smoke & halogen free, suitable for installations on passenger ships, as on other commercial vessels.

Standards

	IEC 60092-350/351/376/359

	IEC 60331-21

	IEC 60332-1

	IEC 60332-3-22

	IEC 60754-1/2

	IEC 61034

Stranded Copper Conductor Mica Tape + XLPE Insulation Al/polyester Tape + Drain Wire LSZH (SHF1) Outer Sheath

Construction

- Conductors: Class 2 stranded copper conductor.

- Insulation: Mica tape + XLPE.

- Cabling Element: Pair/Triple.

- Individual Screen: Al/polyester tape.

- Drain Wire: Tinned copper wire.

- Outer Sheath: LSOH (SHF1). SHF2 can be offered upon request.

Core Identification

Pair: White/blue with printed pair number and core number. Triple: White/blue/red with printed triple number.

www.addison-cables.com

ADDISON	79

IEC Standard Caledonian Offshore & Marine Cables

MariSig Fire Resistant Instrumentation & Control Cables

www.caledonian-cables.co.uk

Mechanical and Thermal Properties

Bending Radius for Fixed Installations: 6×OD (OD>25mm); 4×OD (OD ≤25mm) Temperature Range: -30℃ ~ +80℃

Dimensions and Weight

| Part No. | Construction No. of elements×No. of cores in element×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MRE-M2XH PiMF-1P0.75 | 1×2×0.75 | 0.5 | 1.0 | 7.9 | 80 |
| MRE-M2XH PiMF-2P0.75 | 2×2×0.75 | 0.5 | 1.2 | 12.4 | 170 |
| MRE-M2XH PiMF-3P0.75 | 3×2×0.75 | 0.5 | 1.2 | 13.2 | 210 |
| MRE-M2XH PiMF-4P0.75 | 4×2×0.75 | 0.5 | 1.3 | 14.3 | 260 |
| MRE-M2XH PiMF-5P0.75 | 5×2×0.75 | 0.5 | 1.3 | 16.0 | 320 |
| MRE-M2XH PiMF-6P0.75 | 6×2×0.75 | 0.5 | 1.4 | 17.4 | 380 |
| MRE-M2XH PiMF-7P0.75 | 7×2×0.75 | 0.5 | 1.4 | 17.4 | 410 |
| MRE-M2XH PiMF-8P0.75 | 8×2×0.75 | 0.5 | 1.4 | 18.5 | 460 |
| MRE-M2XH PiMF-10P0.75 | 10×2×0.75 | 0.5 | 1.5 | 21.0 | 570 |
| MRE-M2XH PiMF-12P0.75 | 12×2×0.75 | 0.5 | 1.5 | 21.8 | 650 |
| MRE-M2XH PiMF-14P0.75 | 14×2×0.75 | 0.5 | 1.6 | 22.9 | 740 |
| MRE-M2XH PiMF-16P0.75 | 16×2×0.75 | 0.5 | 1.6 | 24.6 | 840 |
| MRE-M2XH PiMF-19P0.75 | 19×2×0.75 | 0.5 | 1.7 | 26.5 | 980 |
| MRE-M2XH PiMF-20P0.75 | 20×2×0.75 | 0.5 | 1.7 | 26.5 | 1010 |
| MRE-M2XH PiMF-24P0.75 | 24×2×0.75 | 0.5 | 1.9 | 30.6 | 1260 |
| MRE-M2XH PiMF-30P0.75 | 30×2×0.75 | 0.5 | 2.0 | 33.4 | 1530 |
| MRE-M2XH PiMF-37P0.75 | 37×2×0.75 | 0.5 | 2.1 | 35.9 | 1830 |
| MRE-M2XH PiMF-1P1.0 | 1×2×1.0 | 0.5 | 1.0 | 8.3 | 90 |
| MRE-M2XH PiMF-2P1.0 | 2×2×1.0 | 0.5 | 1.2 | 13.1 | 200 |
| MRE-M2XH PiMF-3P1.0 | 3×2×1.0 | 0.5 | 1.3 | 14.2 | 250 |
| MRE-M2XH PiMF-4P1.0 | 4×2×1.0 | 0.5 | 1.3 | 15.1 | 310 |
| MRE-M2XH PiMF-5P1.0 | 5×2×1.0 | 0.5 | 1.4 | 17.1 | 380 |
| MRE-M2XH PiMF-6P1.0 | 6×2×1.0 | 0.5 | 1.4 | 18.4 | 440 |
| MRE-M2XH PiMF-7P1.0 | 7×2×1.0 | 0.5 | 1.4 | 18.4 | 480 |
| MRE-M2XH PiMF-8P1.0 | 8×2×1.0 | 0.5 | 1.5 | 19.8 | 550 |
| MRE-M2XH PiMF-10P1.0 | 10×2×1.0 | 0.5 | 1.6 | 22.4 | 690 |
| MRE-M2XH PiMF-12P1.0 | 12×2×1.0 | 0.5 | 1.6 | 23.3 | 780 |
| MRE-M2XH PiMF-14P1.0 | 14×2×1.0 | 0.5 | 1.6 | 24.2 | 880 |
| MRE-M2XH PiMF-16P1.0 | 16×2×1.0 | 0.5 | 1.7 | 26.3 | 1020 |
| MRE-M2XH PiMF-19P1.0 | 19×2×1.0 | 0.5 | 1.8 | 28.3 | 1190 |

80	ADDISON	www.addison-cables.com

IEC Standard Caledonian Offshore & Marine Cables

MariSig Fire Resistant Instrumentation & Control Cables

www.caledonian-cables.co.uk

| Part No. | Construction No. of elements×No. of cores in element×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MRE-M2XH PiMF-20P1.0 | 20×2×1.0 | 0.5 | 1.8 | 28.3 | 1230 |
| MRE-M2XH PiMF-24P1.0 | 24×2×1.0 | 0.5 | 1.9 | 32.5 | 1510 |
| MRE-M2XH PiMF-30P1.0 | 30×2×1.0 | 0.5 | 2.0 | 35.4 | 1840 |
| MRE-M2XH PiMF-37P1.0 | 37×2×1.0 | 0.5 | 2.1 | 38.1 | 2210 |
| MRE-M2XH TiMF-1T0.75 | 1×3×0.75 | 0.5 | 1.0 | 8.3 | 100 |
| MRE-M2XH TiMF-2T0.75 | 2×3×0.75 | 0.5 | 1.2 | 13.5 | 210 |
| MRE-M2XH TiMF-3T0.75 | 3×3×0.75 | 0.5 | 1.3 | 14.5 | 270 |
| MRE-M2XH TiMF-4T0.75 | 4×3×0.75 | 0.5 | 1.3 | 16.0 | 330 |
| MRE-M2XH TiMF-5T0.75 | 5×3×0.75 | 0.5 | 1.4 | 17.9 | 410 |
| MRE-M2XH TiMF-6T0.75 | 6×3×0.75 | 0.5 | 1.5 | 20.3 | 500 |
| MRE-M2XH TiMF-7T0.75 | 7×3×0.75 | 0.5 | 1.5 | 20.3 | 540 |
| MRE-M2XH TiMF-8T0.75 | 8×3×0.75 | 0.5 | 1.5 | 21.8 | 620 |
| MRE-M2XH TiMF-10T0.75 | 10×3×0.75 | 0.5 | 1.7 | 25.0 | 780 |
| MRE-M2XH TiMF-12T0.75 | 12×3×0.75 | 0.5 | 1.7 | 26.4 | 900 |
| MRE-M2XH TiMF-14T0.75 | 14×3×0.75 | 0.5 | 1.8 | 27.7 | 1020 |
| MRE-M2XH TiMF-16T0.75 | 16×3×0.75 | 0.5 | 1.8 | 29.5 | 1160 |
| MRE-M2XH TiMF-19T0.75 | 19×3×0.75 | 0.5 | 1.9 | 32.0 | 1360 |
| MRE-M2XH TiMF-20T0.75 | 20×3×0.75 | 0.5 | 1.9 | 32.5 | 1420 |
| MRE-M2XH TiMF-24T0.75 | 24×3×0.75 | 0.5 | 2.1 | 35.7 | 1700 |
| MRE-M2XH TiMF-30T0.75 | 30×3×0.75 | 0.5 | 2.2 | 39.6 | 2100 |
| MRE-M2XH TiMF-32T0.75 | 32×3×0.75 | 0.5 | 2.3 | 41.2 | 2250 |
| MRE-M2XH TiMF-1T1.0 | 1×3×1.0 | 0.5 | 1.1 | 8.9 | 120 |
| MRE-M2XH TiMF-2T1.0 | 2×3×1.0 | 0.5 | 1.3 | 14.4 | 250 |
| MRE-M2XH TiMF-3T1.0 | 3×3×1.0 | 0.5 | 1.3 | 15.4 | 310 |
| MRE-M2XH TiMF-4T1.0 | 4×3×1.0 | 0.5 | 1.4 | 17.1 | 400 |
| MRE-M2XH TiMF-5T1.0 | 5×3×1.0 | 0.5 | 1.4 | 18.9 | 480 |
| MRE-M2XH TiMF-6T1.0 | 6×3×1.0 | 0.5 | 1.5 | 21.5 | 590 |
| MRE-M2XH TiMF-7T1.0 | 7×3×1.0 | 0.5 | 1.5 | 21.5 | 640 |
| MRE-M2XH TiMF-8T1.0 | 8×3×1.0 | 0.5 | 1.6 | 23.3 | 740 |
| MRE-M2XH TiMF-10T1.0 | 10×3×1.0 | 0.5 | 1.7 | 26.5 | 930 |
| MRE-M2XH TiMF-12T1.0 | 12×3×1.0 | 0.5 | 1.8 | 28.2 | 1090 |
| MRE-M2XH TiMF-14T1.0 | 14×3×1.0 | 0.5 | 1.8 | 29.4 | 1220 |
| MRE-M2XH TiMF-16T1.0 | 16×3×1.0 | 0.5 | 1.9 | 31.5 | 1400 |
| MRE-M2XH TiMF-19T1.0 | 19×3×1.0 | 0.5 | 2.0 | 34.1 | 1640 |
| MRE-M2XH TiMF-20T1.0 | 20×3×1.0 | 0.5 | 2.0 | 34.7 | 1710 |
| MRE-M2XH TiMF-24T1.0 | 24×3×1.0 | 0.5 | 2.1 | 37.9 | 2040 |
| MRE-M2XH TiMF-30T1.0 | 30×3×1.0 | 0.5 | 2.3 | 42.3 | 2540 |
| MRE-M2XH TiMF-32T1.0 | 32×3×1.0 | 0.5 | 2.4 | 44.0 | 2720 |

www.addison-cables.com

ADDISON	81