MRE-M2XCH 150/250V Mica Tape + XLPE Insulated, LSOH (SHF1) Sheathed, Armoured Fire Resistant Instrumentation & Control Cables (Multipair/Multitriple)

Application

These cables are used on board of ships in all locations for fixed installations complying with IEC standards 60092-352 in safety circuit, where fire resistance is required. These cables are fire resistant, flame retardant, low smoke & halogen free, suitable for installations on passenger ships, as on other commercial vessels.

Standards

	IEC 60092-350/351/376/359

	IEC 60331-21

	IEC 60332-1

	IEC 60332-3-22

	IEC 60754-1/2

	IEC 61034

Stranded Copper Conductor Mica Tape + XLPE Insulation Polyester Tape

Copper Wire Braid Armour LSOH (SHF1) Outer Sheath

Construction

- Conductors: Class 2 stranded copper conductor.

- Insulation: Mica tape + XLPE.

- Cabling Element: Pair/Triple.

- Inner Covering: Lapped polyester tape.

- Armour: Copper wire braid.

- Outer Sheath: LSOH (SHF1). SHF2 can be offered upon request.

Core Identification

Pair: White/blue with printed pair number and core number. Triple: White/blue/red with printed triple number.

Mechanical and Thermal Properties

Bending Radius for Fixed Installations: 6×OD Temperature Range: -30℃ ~ +80℃

Dimensions and Weight

| Part No. | Construction No. of elements×No. of cores in element×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MRE-M2XCH-1P0.75 | 1×2×0.75 | 0.5 | 1.3 | 9.1 | 120 |
| MRE-M2XCH-2P0.75 | 2×2×0.75 | 0.5 | 1.3 | 10.2 | 150 |
| MRE-M2XCH-3P0.75 | 3×2×0.75 | 0.5 | 1.8 | 14.6 | 280 |
| MRE-M2XCH-4P0.75 | 4×2×0.75 | 0.5 | 1.8 | 15.4 | 320 |
| MRE-M2XCH-5P0.75 | 5×2×0.75 | 0.5 | 1.9 | 17.2 | 390 |
| MRE-M2XCH-6P0.75 | 6×2×0.75 | 0.5 | 1.9 | 18.3 | 440 |
| MRE-M2XCH-7P0.75 | 7×2×0.75 | 0.5 | 1.9 | 18.3 | 460 |
| MRE-M2XCH-8P0.75 | 8×2×0.75 | 0.5 | 2.0 | 19.6 | 520 |
| MRE-M2XCH-10P0.75 | 10×2×0.75 | 0.5 | 2.0 | 21.7 | 620 |
| MRE-M2XCH-12P0.75 | 12×2×0.75 | 0.5 | 2.1 | 22.8 | 700 |
| MRE-M2XCH-14P0.75 | 14×2×0.75 | 0.5 | 2.1 | 23.6 | 770 |
| MRE-M2XCH-16P0.75 | 16×2×0.75 | 0.5 | 2.2 | 25.4 | 870 |
| MRE-M2XCH-19P0.75 | 19×2×0.75 | 0.5 | 2.2 | 27.0 | 990 |
| MRE-M2XCH-20P0.75 | 20×2×0.75 | 0.5 | 2.2 | 27.0 | 1010 |
| MRE-M2XCH-24P0.75 | 24×2×0.75 | 0.5 | 2.4 | 30.9 | 1240 |
| MRE-M2XCH-30P0.75 | 30×2×0.75 | 0.5 | 2.5 | 33.5 | 1480 |
| MRE-M2XCH-37P0.75 | 37×2×0.75 | 0.5 | 2.6 | 35.9 | 1730 |
| MRE-M2XCH-1P1.0 | 1×2×1.0 | 0.5 | 1.3 | 9.5 | 130 |
| MRE-M2XCH-2P1.0 | 2×2×1.0 | 0.5 | 1.3 | 10.7 | 170 |
| MRE-M2XCH-3P1.0 | 3×2×1.0 | 0.5 | 1.8 | 15.3 | 320 |
| MRE-M2XCH-4P1.0 | 4×2×1.0 | 0.5 | 1.8 | 16.2 | 360 |
| MRE-M2XCH-5P1.0 | 5×2×1.0 | 0.5 | 1.9 | 18.1 | 440 |
| MRE-M2XCH-6P1.0 | 6×2×1.0 | 0.5 | 2.0 | 19.5 | 510 |
| MRE-M2XCH-7P1.0 | 7×2×1.0 | 0.5 | 2.0 | 19.5 | 530 |
| MRE-M2XCH-8P1.0 | 8×2×1.0 | 0.5 | 2.0 | 20.7 | 590 |
| MRE-M2XCH-10P1.0 | 10×2×1.0 | 0.5 | 2.1 | 23.2 | 730 |
| MRE-M2XCH-12P1.0 | 12×2×1.0 | 0.5 | 2.1 | 24.1 | 810 |
| MRE-M2XCH-14P1.0 | 14×2×1.0 | 0.5 | 2.2 | 25.1 | 900 |
| MRE-M2XCH-16P1.0 | 16×2×1.0 | 0.5 | 2.2 | 26.9 | 1010 |
| MRE-M2XCH-19P1.0 | 19×2×1.0 | 0.5 | 2.3 | 28.8 | 1160 |

| Part No. | Construction No. of elements×No. of cores in element×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MRE-M2XCH-20P1.0 | 20×2×1.0 | 0.5 | 2.3 | 28.8 | 1190 |
| MRE-M2XCH-24P1.0 | 24×2×1.0 | 0.5 | 2.5 | 33.0 | 1460 |
| MRE-M2XCH-30P1.0 | 30×2×1.0 | 0.5 | 2.6 | 35.8 | 1740 |
| MRE-M2XCH-37P1.0 | 37×2×1.0 | 0.5 | 2.9 | 38.8 | 2140 |
| MRE-M2XCH-1P1.5 | 1×2×1.5 | 0.6 | 1.3 | 10.5 | 160 |
| MRE-M2XCH-2P1.5 | 2×2×1.5 | 0.6 | 1.4 | 12.1 | 220 |
| MRE-M2XCH-3P1.5 | 3×2×1.5 | 0.6 | 1.9 | 17.4 | 400 |
| MRE-M2XCH-4P1.5 | 4×2×1.5 | 0.6 | 1.9 | 18.4 | 470 |
| MRE-M2XCH-5P1.5 | 5×2×1.5 | 0.6 | 2.0 | 20.6 | 570 |
| MRE-M2XCH-6P1.5 | 6×2×1.5 | 0.6 | 2.1 | 22.2 | 660 |
| MRE-M2XCH-7P1.5 | 7×2×1.5 | 0.6 | 2.1 | 22.2 | 700 |
| MRE-M2XCH-8P1.5 | 8×2×1.5 | 0.6 | 2.1 | 23.6 | 780 |
| MRE-M2XCH-10P1.5 | 10×2×1.5 | 0.6 | 2.2 | 26.5 | 950 |
| MRE-M2XCH-12P1.5 | 12×2×1.5 | 0.6 | 2.3 | 27.7 | 1070 |
| MRE-M2XCH-14P1.5 | 14×2×1.5 | 0.6 | 2.3 | 28.7 | 1180 |
| MRE-M2XCH-16P1.5 | 16×2×1.5 | 0.6 | 2.4 | 31.0 | 1350 |
| MRE-M2XCH-19P1.5 | 19×2×1.5 | 0.6 | 2.5 | 33.2 | 1560 |
| MRE-M2XCH-20P1.5 | 20×2×1.5 | 0.6 | 2.5 | 33.2 | 1590 |
| MRE-M2XCH-24P1.5 | 24×2×1.5 | 0.6 | 2.9 | 38.5 | 2060 |
| MRE-M2XCH-30P1.5 | 30×2×1.5 | 0.6 | 3.0 | 41.8 | 2450 |
| MRE-M2XCH-37P1.5 | 37×2×1.5 | 0.6 | 3.1 | 44.7 | 2880 |
| MRE-M2XCH-1T0.75 | 1×3×0.75 | 0.5 | 1.3 | 9.5 | 130 |
| MRE-M2XCH-2T0.75 | 2×3×0.75 | 0.5 | 1.8 | 14.9 | 290 |
| MRE-M2XCH-3T0.75 | 3×3×0.75 | 0.5 | 1.8 | 15.7 | 340 |
| MRE-M2XCH-4T0.75 | 4×3×0.75 | 0.5 | 1.9 | 17.2 | 410 |
| MRE-M2XCH-5T0.75 | 5×3×0.75 | 0.5 | 1.9 | 18.8 | 480 |
| MRE-M2XCH-6T0.75 | 6×3×0.75 | 0.5 | 2.0 | 21.2 | 590 |
| MRE-M2XCH-7T0.75 | 7×3×0.75 | 0.5 | 2.0 | 21.2 | 620 |
| MRE-M2XCH-8T0.75 | 8×3×0.75 | 0.5 | 2.1 | 22.8 | 700 |
| MRE-M2XCH-10T0.75 | 10×3×0.75 | 0.5 | 2.2 | 25.7 | 860 |
| MRE-M2XCH-12T0.75 | 12×3×0.75 | 0.5 | 2.2 | 27.0 | 970 |
| MRE-M2XCH-14T0.75 | 14×3×0.75 | 0.5 | 2.3 | 28.3 | 1080 |
| MRE-M2XCH-16T0.75 | 16×3×0.75 | 0.5 | 2.3 | 29.9 | 1200 |
| MRE-M2XCH-19T0.75 | 19×3×0.75 | 0.5 | 2.4 | 32.3 | 1390 |
| MRE-M2XCH-20T0.75 | 20×3×0.75 | 0.5 | 2.5 | 33.0 | 1460 |
| MRE-M2XCH-24T0.75 | 24×3×0.75 | 0.5 | 2.6 | 35.9 | 1710 |
| MRE-M2XCH-30T0.75 | 30×3×0.75 | 0.5 | 2.9 | 40.1 | 2170 |
| MRE-M2XCH-32T0.75 | 32×3×0.75 | 0.5 | 3.0 | 41.7 | 2320 |
| MRE-M2XCH-1T1.0 | 1×3×1.0 | 0.5 | 1.3 | 9.9 | 150 |
| MRE-M2XCH-2T1.0 | 2×3×1.0 | 0.5 | 1.8 | 15.6 | 320 |

| Part No. | Construction No. of elements×No. of cores in element×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MRE-M2XCH-3T1.0 | 3×3×1.0 | 0.5 | 1.8 | 16.5 | 380 |
| MRE-M2XCH-4T1.0 | 4×3×1.0 | 0.5 | 1.9 | 18.1 | 470 |
| MRE-M2XCH-5T1.0 | 5×3×1.0 | 0.5 | 2.0 | 20.1 | 560 |
| MRE-M2XCH-6T1.0 | 6×3×1.0 | 0.5 | 2.1 | 22.6 | 680 |
| MRE-M2XCH-7T1.0 | 7×3×1.0 | 0.5 | 2.1 | 22.6 | 720 |
| MRE-M2XCH-8T1.0 | 8×3×1.0 | 0.5 | 2.1 | 24.1 | 810 |
| MRE-M2XCH-10T1.0 | 10×3×1.0 | 0.5 | 2.2 | 27.2 | 990 |
| MRE-M2XCH-12T1.0 | 12×3×1.0 | 0.5 | 2.3 | 28.8 | 1130 |
| MRE-M2XCH-14T1.0 | 14×3×1.0 | 0.5 | 2.3 | 30.0 | 1260 |
| MRE-M2XCH-16T1.0 | 16×3×1.0 | 0.5 | 2.4 | 31.9 | 1410 |
| MRE-M2XCH-19T1.0 | 19×3×1.0 | 0.5 | 2.5 | 34.4 | 1640 |
| MRE-M2XCH-20T1.0 | 20×3×1.0 | 0.5 | 2.5 | 35.0 | 1700 |
| MRE-M2XCH-24T1.0 | 24×3×1.0 | 0.5 | 2.9 | 38.8 | 2110 |
| MRE-M2XCH-30T1.0 | 30×3×1.0 | 0.5 | 3.0 | 42.8 | 2560 |
| MRE-M2XCH-32T1.0 | 32×3×1.0 | 0.5 | 3.1 | 44.4 | 2730 |
| MRE-M2XCH-1T1.5 | 1×3×1.5 | 0.6 | 1.3 | 11.0 | 180 |
| MRE-M2XCH-2T1.5 | 2×3×1.5 | 0.6 | 1.9 | 17.7 | 410 |
| MRE-M2XCH-3T1.5 | 3×3×1.5 | 0.6 | 1.9 | 18.7 | 490 |
| MRE-M2XCH-4T1.5 | 4×3×1.5 | 0.6 | 2.0 | 20.6 | 610 |
| MRE-M2XCH-5T1.5 | 5×3×1.5 | 0.6 | 2.1 | 22.9 | 740 |
| MRE-M2XCH-6T1.5 | 6×3×1.5 | 0.6 | 2.2 | 25.8 | 890 |
| MRE-M2XCH-7T1.5 | 7×3×1.5 | 0.6 | 2.2 | 25.8 | 950 |
| MRE-M2XCH-8T1.5 | 8×3×1.5 | 0.6 | 2.3 | 27.7 | 1070 |
| MRE-M2XCH-10T1.5 | 10×3×1.5 | 0.6 | 2.4 | 31.3 | 1320 |
| MRE-M2XCH-12T1.5 | 12×3×1.5 | 0.6 | 2.5 | 33.2 | 1520 |
| MRE-M2XCH-14T1.5 | 14×3×1.5 | 0.6 | 2.5 | 34.6 | 1690 |
| MRE-M2XCH-16T1.5 | 16×3×1.5 | 0.6 | 2.8 | 37.3 | 1990 |
| MRE-M2XCH-19T1.5 | 19×3×1.5 | 0.6 | 2.9 | 40.3 | 2310 |
| MRE-M2XCH-20T1.5 | 20×3×1.5 | 0.6 | 3.0 | 41.1 | 2420 |
| MRE-M2XCH-24T1.5 | 24×3×1.5 | 0.6 | 3.1 | 44.7 | 2840 |
| MRE-M2XCH-30T1.5 | 30×3×1.5 | 0.6 | 3.3 | 49.5 | 3460 |
| MRE-M2XCH-32T1.5 | 32×3×1.5 | 0.6 | 3.3 | 51.2 | 3670 |

*: 2 pairs are assembled as a quad.