IEC Standard Caledonian Offshore & Marine Cables

MariFlex Marine Fire Resistant Power & Control Cables

www.caledonian-cables.co.uk

MFX400 0.6/1 kV Mica Tape + XLPE Insulated, LSOH (SHF1) Sheathed, Armoured Fire Resistant Power & Control Cables (Multicore)

Application

These armoured fire resistant cables are used on board of ships in all locations for fixed installations where cable protection is required. These cables are fire resistant, flame retardant, low smoke & halogen free.

Standards

	IEC 60092-350/351/353/359

	IEC 60331-21

	IEC 60332-1

	IEC 60332-3-22

	IEC 60754-1/2

	IEC 61034

Stranded Copper Conductor Mica Tape + XLPE Insulation Extruded Inner Covering Copper Wire Braid Armour LSOH (SHF1) Sheath

Construction

- Conductors: Class 2 stranded copper conductor. Class 5 stranded conductors can be offered upon request.

- Insulation: Mica tape + XLPE.

- Inner Covering: Extruded inner covering.

- Armour: Copper wire braid.

- Outer Sheath: LSOH (SHF1). SHF2 can be offered upon request.

Core Identification

Two cores: Blue, Brown.

Three cores: Brown, Black, Grey. Four cores: Blue, Brown, Black, Grey.

Five cores: Blue, Brown, Black, Grey, Black. Multi cores: White with black numbers.

www.addison-cables.com

ADDISON	37

IEC Standard Caledonian Offshore & Marine Cables

MariFlex Marine Fire Resistant Power & Control Cables

www.caledonian-cables.co.uk

Mechanical and Thermal Properties

Bending Radius for Fixed Installations: 6×OD Temperature Range: -30℃ ~ +80℃

Dimensions and Weight

MFX400 1mRMZ1-R Multicore Armoured 0.6/1kV (-R stands for class 2 conductor. For class 5 conductor, please change –R to –F)

| Part No. | Construction No. of cores×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MFX400-1mRMZ1-R-2C1.5 | 2×1.5 | 0.7 | 1.1 | 10.5 | 180 |
| MFX400-1mRMZ1-R-2C2.5 | 2×2.5 | 0.7 | 1.1 | 11.7 | 230 |
| MFX400-1mRMZ1-R-2C4 | 2×4 | 0.9 | 1.2 | 12.9 | 290 |
| MFX400-1mRMZ1-R-2C6 | 2×6 | 0.9 | 1.2 | 14.8 | 400 |
| MFX400-1mRMZ1-R-2C10 | 2×10 | 0.9 | 1.3 | 16.6 | 570 |
| MFX400-1mRMZ1-R-2C16 | 2×16 | 0.9 | 1.4 | 19.0 | 770 |
| MFX400-1mRMZ1-R-2C25 | 2×25 | 0.9 | 1.5 | 22.8 | 1130 |
| MFX400-1mRMZ1-R-2C35 | 2×35 | 0.9 | 1.5 | 25.0 | 1420 |
| MFX400-1mRMZ1-R-2C50 | 2×50 | 1.0 | 1.5 | 28.0 | 1860 |
| MFX400-1mRMZ1-R-3C1.5 | 3×1.5 | 0.7 | 1.1 | 11.2 | 210 |
| MFX400-1mRMZ1-R-3C2.5 | 3×2.5 | 0.7 | 1.1 | 12.2 | 260 |
| MFX400-1mRMZ1-R-3C4 | 3×4 | 0.9 | 1.2 | 13.5 | 340 |
| MFX400-1mRMZ1-R-3C6 | 3×6 | 0.9 | 1.3 | 15.7 | 480 |
| MFX400-1mRMZ1-R-3C10 | 3×10 | 0.9 | 1.3 | 17.7 | 680 |
| MFX400-1mRMZ1-R-3C16 | 3×16 | 0.9 | 1.4 | 20.0 | 930 |
| MFX400-1mRMZ1-R-3C25 | 3×25 | 0.9 | 1.6 | 24.1 | 1380 |
| MFX400-1mRMZ1-R-3C35 | 3×35 | 0.9 | 1.6 | 26.4 | 1770 |
| MFX400-1mRMZ1-R-3C50 | 3×50 | 1.0 | 1.6 | 29.6 | 2350 |
| MFX400-1mRMZ1-R-3C70S | 3×70 (sector shaped) | 1.1 | 2.0 | 31.9 | 2930 |
| MFX400-1mRMZ1-R-3C95S | 3×95 (sector shaped) | 1.1 | 2.1 | 36.1 | 3870 |
| MFX400-1mRMZ1-R-3C120S | 3×120 (sector shaped) | 1.2 | 2.2 | 39.6 | 4770 |
| MFX400-1mRMZ1-R-4C1.5 | 4×1.5 | 0.7 | 1.1 | 12.1 | 250 |
| MFX400-1mRMZ1-R-4C2.5 | 4×2.5 | 0.7 | 1.2 | 12.9 | 300 |
| MFX400-1mRMZ1-R-4C4 | 4×4 | 0.9 | 1.3 | 15.4 | 440 |
| MFX400-1mRMZ1-R-4C6 | 4×6 | 0.9 | 1.3 | 17.0 | 570 |
| MFX400-1mRMZ1-R-4C10 | 4×10 | 0.9 | 1.4 | 19.1 | 810 |
| MFX400-1mRMZ1-R-4C16 | 4×16 | 0.9 | 1.5 | 22.2 | 1160 |
| MFX400-1mRMZ1-R-4C25 | 4×25 | 0.9 | 1.6 | 26.9 | 1720 |

38	ADDISON	www.addison-cables.com

IEC Standard Caledonian Offshore & Marine Cables

MariFlex Marine Fire Resistant Power & Control Cables

www.caledonian-cables.co.uk

| Part No. | Construction No. of cores×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MFX400-1mRMZ1-R-4C35 | 4×35 | 0.9 | 1.7 | 29.7 | 2220 |
| MFX400-1mRMZ1-R-5C1.5 | 5×1.5 | 0.7 | 1.2 | 12.8 | 280 |
| MFX400-1mRMZ1-R-7C1.5 | 7×1.5 | 0.7 | 1.2 | 14.3 | 370 |
| MFX400-1mRMZ1-R-12C1.5 | 12×1.5 | 0.7 | 1.4 | 17.9 | 570 |
| MFX400-1mRMZ1-R-19C1.5 | 19×1.5 | 0.7 | 1.5 | 20.7 | 790 |
| MFX400-1mRMZ1-R-27C1.5 | 27×1.5 | 0.7 | 1.7 | 24.4 | 1100 |
| MFX400-1mRMZ1-R-37C1.5 | 37×1.5 | 0.7 | 1.9 | 27.3 | 1380 |
| MFX400-1mRMZ1-R-5C2.5 | 5×2.5 | 0.7 | 1.2 | 14.7 | 400 |
| MFX400-1mRMZ1-R-7C2.5 | 7×2.5 | 0.7 | 1.2 | 15.8 | 480 |
| MFX400-1mRMZ1-R-12C2.5 | 12×2.5 | 0.7 | 1.4 | 20.3 | 780 |
| MFX400-1mRMZ1-R-19C2.5 | 19×2.5 | 0.7 | 1.5 | 23.4 | 1070 |
| MFX400-1mRMZ1-R-27C2.5 | 27×2.5 | 0.7 | 1.7 | 27.9 | 1500 |

www.addison-cables.com

ADDISON	39