IEC Standard Caledonian Offshore & Marine Cables

MariFlex Marine Fire Resistant Power & Control Cables

www.caledonian-cables.co.uk

MFX400 0.6/1 kV Fire Barriers + HEPR Insulated, LSOH (SHF1) Sheathed, Screened Fire Resistant Power & Control Cables (Multicore)

Application

These cables are used for fixed installations fixed installations on ships and offshore units in all locations and on open deck in safety circuits, where fire resistance is required. The good screening qualities of the copper braid also reduce radio interference and electrical influences to electronics installations. These cables are fire resistant, flame retardant, low smoke & halogen free.

Standards

	DIN 89160/98

	IEC 60092-353

	IEC 60331-21

	IEC 60332-1

	IEC 60332-3-22

	IEC 60754-1/2

	IEC 61034

Stranded Copper Conductor Fire Barriers + HEPR Insulation Lapping/Extruded Filler

Copper Wire Braid Screen LSOH (SHF1) Sheath

Construction

- Conductors: Class 2 stranded copper conductor.

- Insulation: Fire barriers + HEPR.

- Inner Covering: Lapping or extruded filler.

- Overall Screen: Copper wire braid.

- Outer Sheath: LSOH (SHF1).

Core Identification

Two cores: Black, Blue.

Three cores: Black, Blue, Brown.

Four cores: Black, Blue, Brown, Black.

Five cores: Black, Blue, Brown, Black, Black.

42	ADDISON	www.addison-cables.com

IEC Standard Caledonian Offshore & Marine Cables

MariFlex Marine Fire Resistant Power & Control Cables

www.caledonian-cables.co.uk

Multi cores: All cores natural coloured, printed with numbers, starting in center with number 1. Cables with 3 cores and more also with green/yellow core (has to be stated in order).

Mechanical and Thermal Properties

Bending Radius for Fixed Installations: 6×OD Temperature Range: -20℃ ~ +75℃

Dimensions and Weight

| Part No. | Construction No. of cores×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Sheath Thickness mm | Nominal Overall Diameter mm | Nominal Weight kg/km |
| --- | --- | --- | --- | --- | --- |
| MFX400-1mG7MZ1-R-2C1.5 | 2×1.5 | 0.7 | 1.2 | 12.5 | 210 |
| MFX400-1mG7MZ1-R-2C2.5 | 2×2.5 | 0.7 | 1.2 | 13.0 | 250 |
| MFX400-1mG7MZ1-R-2C4 | 2×4 | 0.7 | 1.3 | 14.0 | 300 |
| MFX400-1mG7MZ1-R-2C6 | 2×6 | 0.7 | 1.3 | 16.0 | 410 |
| MFX400-1mG7MZ1-R-2C10 | 2×10 | 0.7 | 1.4 | 18.0 | 550 |
| MFX400-1mG7MZ1-R-2C16 | 2×16 | 0.7 | 1.5 | 20.0 | 720 |
| MFX400-1mG7MZ1-R-2C25 | 2×25 | 0.9 | 1.6 | 23.5 | 1050 |
| MFX400-1mG7MZ1-R-3C1.5 | 3×1.5 | 0.7 | 1.2 | 13.0 | 230 |
| MFX400-1mG7MZ1-R-3C2.5 | 3×2.5 | 0.7 | 1.2 | 14.0 | 280 |
| MFX400-1mG7MZ1-R-3C4 | 3×4 | 0.7 | 1.3 | 15.0 | 350 |
| MFX400-1mG7MZ1-R-3C6 | 3×6 | 0.7 | 1.3 | 16.5 | 480 |
| MFX400-1mG7MZ1-R-3C10 | 3×10 | 0.7 | 1.4 | 19.0 | 670 |
| MFX400-1mG7MZ1-R-3C16 | 3×16 | 0.7 | 1.5 | 21.0 | 870 |
| MFX400-1mG7MZ1-R-3C25 | 3×25 | 0.9 | 1.7 | 24.5 | 1300 |
| MFX400-1mG7MZ1-R-3C35 | 3×35 | 0.9 | 1.8 | 27.0 | 1680 |
| MFX400-1mG7MZ1-R-3C50 | 3×50 | 1.0 | 2.1 | 30.5 | 2190 |
| MFX400-1mG7MZ1-R-3C70 | 3×70 | 1.1 | 2.0 | 35.0 | 3020 |
| MFX400-1mG7MZ1-R-3C95 | 3×95 | 1.1 | 2.3 | 39.5 | 4050 |
| MFX400-1mG7MZ1-R-3C120 | 3×120 | 1.2 | 2.5 | 44.0 | 5000 |
| MFX400-1mG7MZ1-R-4C1.5 | 4×1.5 | 0.7 | 1.2 | 13.5 | 270 |
| MFX400-1mG7MZ1-R-4C2.5 | 4×2.5 | 0.7 | 1.3 | 15.0 | 330 |
| MFX400-1mG7MZ1-R-4C4 | 4×4 | 0.7 | 1.3 | 16.5 | 460 |
| MFX400-1mG7MZ1-R-4C6 | 4×6 | 0.7 | 1.4 | 18.0 | 560 |
| MFX400-1mG7MZ1-R-4C10 | 4×10 | 0.7 | 1.5 | 20.5 | 790 |
| MFX400-1mG7MZ1-R-4C16 | 4×16 | 0.7 | 1.6 | 23.0 | 1090 |
| MFX400-1mG7MZ1-R-4C25 | 4×25 | 0.9 | 1.8 | 27.0 | 1630 |
| MFX400-1mG7MZ1-R-5C1.5 | 5×1.5 | 0.7 | 1.3 | 14.5 | 320 |
| MFX400-1mG7MZ1-R-5C2.5 | 5×2.5 | 0.7 | 1.3 | 16.5 | 440 |
| MFX400-1mG7MZ1-R-7C1.5 | 7×1.5 | 0.7 | 1.3 | 16.5 | 400 |
| MFX400-1mG7MZ1-R-10C1.5 | 10×1.5 | 0.7 | 1.3 | 19.5 | 450 |
| MFX400-1mG7MZ1-R-12C1.5 | 12×1.5 | 0.7 | 1.4 | 20.0 | 510 |
| MFX400-1mG7MZ1-R-14C1.5 | 14×1.5 | 0.7 | 1.4 | 21.0 | 570 |
| MFX400-1mG7MZ1-R-16C1.5 | 16×1.5 | 0.7 | 1.4 | 22.0 | 640 |
| MFX400-1mG7MZ1-R-19C1.5 | 19×1.5 | 0.7 | 1.5 | 23.5 | 730 |
| MFX400-1mG7MZ1-R-24C1.5 | 24×1.5 | 0.7 | 1.6 | 27.0 | 910 |

www.addison-cables.com

ADDISON	43