BS 6883&BS 7917 Caledonian Offshore & Marine Cables

Fire Resistant Instrumentation & Control Cables

www.caledonian-cables.co.uk

150/250V HF-EPR Insulated, SW2/SW4 Sheathed, Collectively Screened Armoured Fire Resistant Instrumentation & Control Cables

Application

These ﬁre resistant elastomeric insulated cables are designed for ﬁxed wiring in ships and on mobile offshore units, suitable for use in instrumentation, lighting and control circuits where ﬁre integrity is essential.

Standards

	BS 7917

- IEC 60331-31 Fire resistant

- IEC 60332-3A Flame retardant

	IEC 60754-1; IEC 60754-2

Corrosivity

- IEC 61034-2 Smoke density

- Cold bend and impact (-40°C) (on request)

- CSA C22.2 No. 38-95 (on request)

Construction

Stranded Tinned Copper Conductor Mica Tape+HF-EPR GP4 Insulation Aluminium/Polyester Tape + Drain Wire SB1 Inner Sheath

Galvanized Steel Wire Braid SW2/SW4 Outer Sheath

- Conductor: Tinned copper wire stranded circular cl. 2 BS 6360/IEC 60228.

- Insulation: Mica tape + HF-EPR GP4 according to BS 7655 1.2.

- Lay-up: Pairs, triples.

- Collective Screen: Aluminium/polyester tape + drain wire tinned copper.

- Inner Sheath: Halogen free thermosetting compound SB1 according to BS 7917.

- Armour: Galvanized steel wire braid. Tinned bronze wire braid can be offered upon request.

- Outer Sheath: Halogen free thermosetting compound SW4 according to BS 7655 2.6 or reduced halogen thermosetting compound SW2 according to BS 7655 2.6.

44	ADDISON	www.addison-cables.com

BS 6883&BS 7917 Caledonian Offshore & Marine Cables

Flire Resistant Instrumentation & Control Cables

www.caledonian-cables.co.uk

Mechanical and Thermal Properties

Minimum Internal Bending Radius: 8×OD Temperature Range: -40℃ ~ +90℃

Dimensions and Weight

| Construction No. of cores×Cross section(mm²) | Nominal Insulation Thickness mm | Nominal Inner Sheath Thickness mm | Minimum Diameter Over Inner Sheath mm | Maximum Diameter Over Inner Sheath mm | Nominal Armour Wire Diameter mm | Nominal Outer Sheath Thickness mm | Minimum Overall Diameter mm | Maximum Overall Diameter mm | Approx. Weight kg/km |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Multipair |  |  |  |  |  |  |  |  |  |
| 3×2×0.75 | 0.8 | 1.2 | 14.0 | 16.0 | 0.3 | 1.4 | 18.1 | 20.5 | 450 |
| 7×2×0.75 | 0.8 | 1.4 | 18.6 | 20.7 | 0.3 | 1.5 | 22.9 | 25.8 | 720 |
| 12×2×0.75 | 0.8 | 1.6 | 24.4 | 27.0 | 0.3 | 1.7 | 29.1 | 32.7 | 1080 |
| 20×2×0.75 | 0.8 | 1.8 | 30.8 | 34.0 | 0.45 | 2.0 | 36.8 | 40.7 | 1480 |
| 27×2×0.75 | 0.8 | 1.9 | 35.0 | 38.4 | 0.45 | 2.2 | 41.4 | 45.9 | 2140 |
| 37×2×0.75 | 0.8 | 2.1 | 38.8 | 42.6 | 0.45 | 2.3 | 45.4 | 50.1 | 2710 |
| 3×2×1 | 0.8 | 1.2 | 14.8 | 16.8 | 0.3 | 1.4 | 18.9 | 21.3 | 460 |
| 7×2×1 | 0.8 | 1.4 | 19.6 | 22.0 | 0.3 | 1.6 | 24.1 | 27.1 | 780 |
| 12×2×1 | 0.8 | 1.6 | 25.8 | 28.5 | 0.3 | 1.8 | 30.7 | 34.4 | 1170 |
| 20×2×1 | 0.8 | 1.8 | 32.6 | 35.8 | 0.45 | 2.1 | 38.8 | 43.2 | 1860 |
| 27×2×1 | 0.8 | 2.0 | 37.3 | 40.8 | 0.45 | 2.2 | 43.7 | 48.3 | 2330 |
| 37×2×1 | 0.8 | 2.2 | 41.3 | 45.2 | 0.45 | 2.4 | 48.1 | 53.3 | 2980 |
| Multitriple |  |  |  |  |  |  |  |  |  |
| 3×3×0.75 | 0.8 | 1.3 | 15.0 | 17.0 | 0.3 | 1.4 | 19.1 | 21.5 | 510 |
| 7×3×0.75 | 0.8 | 1.4 | 20.5 | 23.0 | 0.3 | 1.6 | 25.1 | 28.1 | 810 |
| 12×3×0.75 | 0.8 | 1.7 | 25.6 | 28.3 | 0.45 | 1.9 | 31.4 | 35.1 | 1370 |
| 3×3×1 | 0.8 | 1.3 | 15.8 | 17.8 | 0.3 | 1.5 | 20.1 | 22.9 | 550 |
| 7×3×1 | 0.8 | 1.5 | 21.9 | 24.4 | 0.3 | 1.7 | 26.6 | 29.7 | 910 |
| 12×3×1 | 0.8 | 1.7 | 27.1 | 29.8 | 0.45 | 2.0 | 33.1 | 36.9 | 1510 |

www.addison-cables.com

ADDISON	45